Challenges faced during manufacturing long cylindrical level probe pockets for sodium technology applications

T. V. Maran*, Vibhav Prajapati, A. Clement, Prem J., Rakesh Kumar Mourya, V. Vinod

Fast Reactor Technology Group, Indira Gandhi Centre for Atomic Research,

Kalpakkam, Tamil Nadu - 603102, India

*Author E-mail: mars@igcar.gov.in

ABSTRACT

Sodium Technology Complex (STC) building is constructed with a high bay (43 m) to meet in-sodium testing of long reactor components. The facility features long vertical test vessels and hence requires long-level probes to measure the sodium level in test vessels. Level probes are kept in the level probe pocket assembly to prevent direct contact with sodium, ensuring their proper functionality. Manufacturing of Level Probe Pocket Assemblies (to have Mutual Inductance type level probes to measure sodium level in vessel, Qty. 17 nos) for the STC was executed at the Zonal Workshop of IGCAR. The assemblies feature a 6-meter-long central pipe, incorporating a pocket closure cup, a 1¼” schedule 10 pipe, a pocket flange, a top flange, and a dummy flange. All parts are meticulously machined, welded, and undergo None Destructive Examination (NDE), then assembled, tested pneumatically, and subjected to Helium Leak Testing (HLT) testing. The Gas Tungsten Arc Welding (GTAW) process was employed to join the closure cup at one end and the pocket/top flange at the other end. To address the high linear distortion potential due to the long pipe length, Multi-pass GTAW with controlled heat input was adopted, which was further supported by intermittent cooling, external clamping fixtures secured at various points using a dial gauge, and continuous purging of the weld zone from the inner side of the pipe to reduce thermal stresses and maintain straightness. Straightness of the pocket is essential to minimising error in the sodium level measurement. Liquid Penetrant Examination (LPE) is performed on the prepared weld edge, root pass and final pass of all the weld joints. Radiographic Examination is performed on all butt joints. Pneumatic testing was performed to ensure the structural integrity of manufactured assemblies. Bubble leak test and HLT are performed to confirm the leak tightness required for sodium technology. Rigorous precautions were taken throughout the welding process to minimise distortion, ensuring compliance with the design specifications. The completed assemblies were thoroughly inspected and validated for seamless probe insertion, meeting all required standards. This approach emphasises the effective integration of advanced welding techniques and stringent testing protocols, ensuring the reliable quality that meets the precision manufacturing requirements of equipment for STC.

Keywords: Level Probe Pocket Assembly, Manufacturing challenges, weld distortion control