EXPERIENCE GAINED DURING HARDFACING, MACHINING AND ASSEMBLY OF TRANSFER POT COMPONENTS FOR PFBR

T. Saravanan1, S. Murugan1, Aniket Singhewad1, K. Narayanan1, S. Surendar Kumar1                        M. Nimala Sundaran2,  Sudhakar Naik3, M. Krishnamoorthy1

B. S. Ramesh Babu1, V. Praveen Kumar1 and Utpal Borah1

1Central Workshop Division, Engineering Services Group

2Components Handling Mechanisms Division, Reactor Design Group

3Sudhakar Naik, QA-BHAVINI

Indira Gandhi Centre for Atomic Research (IGCAR), Kalpakkam-603102

Email: tsn@igcar.gov.in & Mobile No.: 09444638466

Abstract

This paper describes the experience gained during the hardfacing of intricate geometrical shapes of transfer pot components for Prototype Fast Breeder Reactor (PFBR). Transfer pot is an intermediate containment vessel meant for transferring the fuel sub assemblies to/from the reactor core. Transfer pot is an assembly of three major sub-assemblies viz. Pot body assembly, Top guide assembly and bottom guide assembly. The transfer pot has a top guide for subassembly entry and a bottom conical seat on which the subassembly rests. An array of disc springs are provided to accommodate shock load, if any, during sub assembly transfer.

Hardfacing of transfer pot components namely, Guide, Top support plate, Bottom housing, Sub assembly seating Block, and Bottom guide block involves, preparation of QAP, positive material identification of raw materials, qualification of raw materials (AISI 316LN) and hardfacing consumable (AWS SFA 5.21, ERNiCrB), development of WPS and PQR for hardfacing.  The weld  parameters were optimized to achieve Fe-level in hard faced layer as per PFBR specification after many trail  depositions were carried out with single / two layers, different current as well as powder feed rate.   The raw material cutting, annealing at 1050 deg.C, ROH : 150 deg. C/hr., Furnace cooling upto 900 deg.C with ROC : 150 deg.C/hr., pre-machining with allowance followed by dimensional inspection, visual examination, LPE, surface hardness measurement, pre-heating at 500-550 deg. C with uniquely designed enclosure, hard facing by plasma transferred arc process with 550 deg.C  inter-pass temperature, post heating at 550 deg.C and slow cooling to room temperature. Visual examination, LPE, proof machining of harfaced surface to facilitate UT, Stress relieving heat treatment at 750-850 deg. C, visual inspection, ultrasonic testing, and surface hardness measurement using portable hardness tester. The extracted of production test coupons (PTCs) were subjected to destructive testing including, coating thickness, surface hardness, chemical composition of coating surface, micro hardness along the coating as well as across the coating, microstructure at 50X and 500 X.  The hard faced component precisely machined and dimension inspected.  Hardfaced surfaces were subjected to liquid penetrant inspection and Ultrasonic testing. Intricate shapes of the components and PTCs were cut using CNC wire EDM cutting process. Surface treatment of machined and fabricated parts, assembly, welding and Non Destructive Examinations (NDEs). A special fixture was used during the assembly of the hardfaced components, aligned and welded using gas tungsten arc welding process, distortion control techniques were employed and thus weld distortion was proficiently controlled to a larger extent to achieve the required straightness.  The straightness of the Pot body assembly was measured using optical jig transit and achieved the straightness of 1.6mm over the length of  3766 mm. Concentricity of hard-faced and finish machined components were achieved within 0.050 mm. In the assembly, critical requirement of achieving overall length 4083 mm and measurement of lateral movement of the pot body bottom end with and without top cover were checked successfully meeting the stringent PFBR specifications.

Keywords : PFBR transfer pot, pre-heating, PTA hard facing, post heating, Stress relieving Heat Treatment, PTCs, proof machining, hardness measurement, GTAW, Geometrical tolerance, ultrasonic testing, liquid penetrant testing.