Influence of Deposition Parameters on Segregation-Induced Strain in

Ni-Cr-B-Si Hardfaced Coating

N Sreevidya1, 2 *, Hemant Kumar1, C. R. Das1, 3, M. Vasudevan1, 3, and Tom Mathews2, 3, 4

1Indira Gandhi Centre for Atomic Research, Kalpakkam, 603102, India

2University of Madras, Chepauk, Chennai-600 005, India

3A CI of Homi Bhabha National Institute, Kalpakkam 603 102, Tamil Nadu, India

4Indira Gandhi Centre for Atomic Research, Kalpakkam, 603102, India (Retd.)

*Corresponding author email: sreevidya@igcar.gov.in

Abstract

Ni-Cr-B-Si alloy is extensively used for hardfacing of austenitic stainless steel (SS) components of sodium cooled fast reactors to avoid self-welding and galling. In the present work, a 316L(N) stainless steel plate is hardfaced with this alloy using the Plasma Transferred Arc Welding (PTAW) process. During initial deposition, 120 A current is employed. No surface cracks and debonding are observed in the obtained coating as examined by dye penetrant and ultrasonic tests, respectively. However, the coating microstructure appeared to be hypereutectic along with segregation of elements like Fe and Si. In addition, localized distribution of strain is also observed in the coating through Kernel Average Misorientation (KAM) measurement, with the maximum value of KAM being ~4°. Subsequently, a second coating is made using a higher deposition current of 150 A, keeping other parameters constant with the intention of increasing heat input. This resulted in an increase of percentage Fe dilution of the coating from 16.9 to 27.4 and reduction in microhardness from 536±33 HV0.5 to 392±15 HV0.5. Further, microstructure changed to eutectic with reduced elemental segregation. These microstructural and microchemical variations resulting from increased dilution are found to play a role in reducing the maximum KAM value to ~1.8°, indicating the reduction of locally strained regions over the coating. Characterization methods employed include optical, scanning electron and magnetic force microscopies; energy dispersive and Raman spectroscopies; X ray and electron backscatter diffraction; and Thermo Calc simulation. Results from the study reveal that Fe dilution of the Ni-Cr-B-Si hardfaced coating by the SS substrate resulting from variation in deposition parameters affect the strain distribution in the coating, which is specifically attributed to its influence in reducing the precipitation of primary borides, and the related Fe and Si concentration gradient developed during solidification.

Key words: Ni-Cr-B-Si coating, PTAW, dilution, microstructure, EBSD, strain