EFFECT OF SILCON CONTENT IN THE WIRE ON MECHANICAL PROPERTIES AND MICROSTRUCTURAL CHARACTERISTICS OF WIRE ARC ADDITIVE MANUFACTURED CYLINDRICAL COMPONENTS OF ALUMINIUM ALLOYS

¹R.Sudalaimani*, ²V.Balasubramanian, ³S.Malarvizhi

¹Research Scholar, ²‚³ Professor

¹,²‚³Centre for Materials Joining and Research (CEMAJOR),

Department of Manufacturing Engineering,

Annamalai University, Annamalai Nagar-608002

*Email: rsudalaimanime@gmail.com

Abstract: Aluminium and its alloys are widely used in aerospace, automotives engines, transportation and structural applications. The engineering industry is developing the Wire Arc Additive Manufacturing (WAAM) technique to produce near net shape engineering components, which have complex shape and profile. WAAM Process predominantly uses gas metal arc welding (GMAW) technique. An advanced variant of GMAW process, known as cold metal transfer arc welding (CMTAW) technique provides higher deposition rate and low heat input. The central aim of this investigation is to understand the effect of silicon content in the wire on surface quality, dimensional accuracy and internal structure (mechanical and metallurgical) of cylindrical components built with AA4043 and AA1100 alloys using WAAM.

A cylindrical component was built using 1.2mm dia ER 4043 wire through layer by layer deposition. Initially the cylindrical components of size 150 mm height × 150 mm diameters were manufactured by GMAW and CMTAW processes using CMT 4000R welding machine. The cylindrical components were cut into two regions from substrate to 75 mm height (bottom region) and from 75 mm to 150 mm height (top region) and specimen were extracted as per ASTM standards.

The effect of silicon content on the tensile properties and hardness of the cylindrical components were analyzed along building direction. Mechanical testing revealed that AA4043 owing to its high silicon content exhibited improved tensile strength and reduced porosity, while AA1100 demonstrated superior ductility. Micro structural analysis identified columnar and equiaxed dendritic structures with rain refinement highly dependent on cooling rate and alloy composition

Keywords: Wire arc additive manufacturing, Aluminium alloy, Gas metal arc welding, Cold metal transfer arc welding, Mechanical properties