Fatigue Performance of Rotating Arc Welded Quenched and Tempered (Q&T) Steel used in Combat Vehicles (CVs)

1R.Rajpradeep, 2S. Malarvizhi,  3V. Balasubramanian, 4A.HafeezurRahman

*1Research Scholar, 2Professor, 3Professor and Director, 4Scientist – F,

1,2,3Centre for Materials Joining and Research (CEMAJOR)

Department of Manufacturing Engineering,

Annamalai University, Annamalainagar.

4.Combat Vehicles Research & Development Establishment (CVRDE), DRDO, Chennai.

### *Email: rrp.deep@gmail.com

Abstract:

Quenched and tempered (Q&T) steels are vital for combat vehicle construction, where the fatigue performance of welded joints dictates operational durability. This study investigates the potential of Rotating Arc Gas Metal Arc Welding (RA-GMAW) to enhance the fatigue life of these critical components compared to Linear  Gas Metal Arc Welding (LA-GMAW).

The Joints were fabricated using optimized parameters with a low-hydrogen ferritic filler wire. Mechanical properties were characterized through tensile, impact, and hardness tests. Fatigue performance was evaluated under cyclic loading to generate S-N curves, which were benchmarked against IIW recommendations. The Microstructural analysis and fractography were employed to correlate weld integrity with failure mechanisms.

The RA-GMAW process produced joints with a 15% higher fatigue strength and lower notch sensitivity than LA-GMAW. This superiority is attributed to a refined microstructure in the weld metal, characterized by acicular ferrite and lower bainite, which mitigates HAZ softening. The RA-GMAW is a superior welding process for combat vehicle manufacturing, offering enhanced fatigue resistance and structural reliability for armored components.

Keywords: Gas Metal Arc Welding, Rotating Gas Metal Arc Welding, Quenched and Tempered Steels, Fatigue Properties, Microstructure, SN curve