Effect of Forging Pressure on Mechanical Properties and Microstructural Characteristics of Linear Friction Welded         Ti-6Al-4V Alloy Joints

P. Sivaraja*, S. Malarvizhib V. Balasubramanianc, Vijay Petley d, Shweta Vermae

a,b,c   Associate Professor, Professor, Centre for Materials Joining and Research (CEMAJOR), Department of Manufacturing Engineering, Annamalai University, Annamalai Nagar - 608 002, Tamil Nadu,

d,e Gas Turbine Research Establishment (GTRE), Bengaluru - 560093, Karnataka.

*Email: cemajorsiva@gmail.com

ABSTRACT

Linear friction welding (LFW) is an advanced solid-state joining technique increasingly used for fabricating titanium alloy components in aero-engine blisk assemblies. This study investigates the influence of forging pressure on the microstructural evolution and tensile behaviour of Ti-6Al-4V (Ti64) linear friction welded joints. Welding experiments were conducted by varying the forging pressure between 5 and 15 MPa while keeping all other parameters constant. Microstructural characterization using optical and scanning electron microscopy revealed the formation of a fine α+β microstructure in the weld centre (fully deformed zone), while the thermomechanically affected zone exhibited elongated and reoriented α grains along the direction of material flow. The heat-affected zone (HAZ) remained minimal due to the high thermal stability of Ti64 below 800 °C. Mechanical testing indicated that the tensile strength increased with forging pressure up to 10 MPa (maximum strength of 991 MPa and hardness of 440 HV), beyond which it declined due to excessive flash and misalignment. All failures occurred between the TMAZ and HAZ, corresponding to the region of lowest hardness. The results demonstrate that optimizing the forging pressure is critical to achieving a balance between joint strength and microstructural integrity in LFW

Ti-6Al-4V components.
Keywords: Ti-6Al-4V alloy, Linear Friction Welding, Forging Pressure, Microstructures and Microhardness.