INVESTIGATIONS ON THE INTERFACE MICROSTUCTURE CHARACTERISTICS OF Al-Cu DISSIMILAR JOINT MANUFACTURED BY MAGNETIC PULSE WELDING TECHNIQUE

R. Chandrakumar1*, P. Sivaraj2, S. Malarvizhi3, V. Balasubramanian3& V. Suresh4 and C.Bhavanisankar5

1* Research Scholar, 2 Associate Professor, 3 Professor

1, 2, 3Centre for Materials Joining and Research, Annamalai University

4, 5 Magpulse Technologies Pvt. Lt., Bangalore.

*Email: chandru.msr92@gmail.com

ABSTRACT

Magnetic Pulse Welding (MPW) is an essential solid state welding process for joining of dissimilar metals. The present study aimed to join aluminum (AA 1050) and copper (Cu 99.96%) sheets of thickness 0.9 mm each by using MPW. The high velocity collision and jetting are the most important aspect of MPW controlled by welding parameter such as discharge voltage (kV), stand-off distance (mm) and working length (mm). The collision surfaces of Cu and Al, the interface of welding and fracture surface were examined by optical microscope and SEM equipped with EDS analysis.

The results revealed that the good metallurgical bonding was obtained while using discharge voltage of 11.00 kV, air gap of 1.9 mm and working length of 11.00 kV, 1.9 mm and 3 mm whereas higher discharge voltage (beyond 12.00 kV) and air gap (beyond 2.1 mm) result in debonding due to higher impact energy. Changing discharge voltage and stand-off distance can influence the collision velocity, leading to the formation of various types of welding interface with wavy, molten wavy and porous morphologies. The feature of collision surfaces depends on the physical properties of Al and Cu, the variation of collision angle and distance from the centreline of the collision. The two distinct zones: a high-shear zone near the collision centreline (Zone 1) and a low-shear zone near the bond edge (Zone 2) were identified. The AlCu intermetallic compound was predominantly formed in the high-shear zone. The formation mechanism of these intermetallic compounds is attributed to solid-state diffusion, as no signs of melting were detected in the transition zones of the bonding interface, except in the porous zone. Additionally, the bonding interface exhibited higher strength compared to the base metals of Al.

Keywords: Magnetic Pulse welding, Al-Cu dissimilar joint, Collision velocity, Metallurgical and Morphology of weld interface, Intermetallic compounds.