Thermomechanical Analysis of Resistance Spot Welding between DP800 and AISI 1080 Steels Using a Fully Coupled ANSYS Simulation Model

Sabarivasan1*, Sivaraj P1, Prabhakaran B1,Balasubramanian V1

1Centre for Materials Joining and Research (CEMAJOR), Department of Manufacturing Engineering, Annamalai University, Annamalai Nagar, Chidambaram-608002, Tamil Nadu, India.

Annamalai University, Annamalainagar – (P.O), Tamilnadu (State), India – 608002.                                                                                                  Email: vasansabari1996@gmail.com

Abstract

Resistance Spot Welding (RSW) is a widely accepted technique for joining advanced high-strength steels (AHSS) and medium carbon steels in automotive and structural applications. However, dissimilar welding of steels such as DP800 and AISI 1080 poses significant challenges due to variations in their thermal and metallurgical responses. In this study, a fully coupled thermomechanical simulation model was developed using ANSYS software to analyze the temperature distribution, phase transformation, and mechanical behavior during the RSW of DP800 and AISI 1080 steels.

The simulation results were validated with experimental observations to optimize process parameters and predict weld performance. A defect-free weld was achieved under optimized conditions of 6 kA welding current, 4 s welding time, and 0.4 MPa electrode force. The rapid cooling rate of approximately 1200 °C/s promoted complete austenitization during heating and subsequent martensitic transformation upon cooling, yielding a predominantly lath martensitic microstructure in the weld nugget. The intercritical and subcritical heat-affected zones (HAZ) displayed heterogeneous microstructures comprising ferrite and martensite–austenite (M/A) constituents due to incomplete austenitization. Mechanical evaluation confirmed that the nugget zone exhibited higher hardness (~570 HV) owing to the formation of martensite, while the HAZ showed a gradual decrease in hardness away from the fusion line.

The developed ANSYS model effectively predicted the temperature field, phase evolution, and hardness gradient, providing strong correlation with experimental data. The observed asymmetry in microstructural evolution across the weld influenced both the strength–toughness relationship and potential crack initiation near the fusion boundary.

Keywords: Resistance Spot Welding, DP800, AISI 1080, Thermomechanical Simulation, ANSYS, Microstructure, Hardness.