OPTIMIZING AND EVALUATION OF FRICTION STIR PROCESSING PARAMETERS FOR LM25 ALUMINIUM ALLOY WITH 10% SIC PARTICLES USING RESPONSE SURFACE METHODOLOGY TECHNIQUE

1G. Senthilkumaran, 2I. Rajkumar, 3P. Vijayavel*, 4 V. Balasubramanian

1and 2Assistant Professor, 3 and 4Professor

1Department of Computer Sciences and Engineering, Meenakshi Ramaswamy Engineering College, Trichy Main Road, M R Nagar,

Thathanur. 621 804, Tamil Nadu, India. 2Department of Mechanical Engineering, P.S.V College of Engineering & Technology, Mittapalli, Balinayanapalli, Elathagiri (Post)Krishnagiri District, Tamil Nadu India. 3Department of Mechanical Engineering, Meenakshi Ramaswamy Engineering College, Trichy Main Road, M R Nagar, Thathanur. 621 804, Tamil Nadu, India,4Centre for Materials Joining and Research (CEMAJOR) Department of Manufacturing Engineering, Annamalai University, Annamalai Nagar - 608 002. Tamil Nadu, India.

*Email: vijayavelfsp@gmail.com

Abstract

Present investigation focuses on the mechanical properties and microstructural behavior of LM25 aluminium alloy based reinforced with 10% SiCp metal matrix composites by applying the Friction Stir Processing (FSP) technique. Response surface methodology was used to find the FSP optimal process parameters. The experiment used the expected best process parameters, which confirmed the predicted highest value for the mechanical characteristics. Tool rotation speed, Tool traverse speed and Shoulder diameter to pin diameter are the main factors affecting LM25 aluminum alloy-based metal matrix composite. Hence, this experiment examined the effects of five different tool rotation speeds, in particular 600, 700, 800, 900, and 1000 rpm. FSPed samples are fabricated wherein the stir zone mainly contains SiCp. The results indicate rotational speed of 800 rpm as the optimal process parameter and has a significant impact on the wear rate, microstructure and microhardness. Specifically, it was observed that the stirred zone exhibited enhanced wear resistance compared to other parameter stir zones. the findings revealed that after implementing friction stir processing (FSP), a well-defined stir zone was observed on the advancing side (AS) of the stir zone. Furthermore, it is found that the uniform dispersion and strong bonding of SiCp with aluminium alloy metal matrix composites enhance wear resistance.

Keywords: Metal Matrix Composites; Response Surface Methodology method; Friction Stir Processing; Wear properties; Microstructure; Microhardness