INFLUENCE OF PIN VOLUME RATIO ON MICROSTRUCTURE, TENSILE PROPERTIES AND WEAR CHARACTERISTICS OF FRICTION STIR PROCESSED ALUMINIUM BASED METAL MATRIX COMPOSITES

1P. Vijayavel*, 2I. Rajkumar, 3G. Senthilkumaran, 4 V. Balasubramanian

1Professor, 2,3Assistant Professor, 4Professor

1Department of Mechanical Engineering, Meenakshi Ramaswamy Engineering College, Trichy Main Road, M R Nagar,

Thathanur. 621 804, Tamil Nadu, India. 2Department of Mechanical Engineering, P.S.V College of Engineering & Technology, Mittapalli, Balinayanapalli, Elathagiri (Post)Krishnagiri District, Tamil Nadu India. 3Department of Computer Sciences and Engineering, Meenakshi Ramaswamy Engineering College, Trichy Main Road, M R Nagar, Thathanur. 621 804, Tamil Nadu, India,4Centre for Materials Joining and Research (CEMAJOR) Department of Manufacturing Engineering, Annamalai University, Annamalai Nagar - 608 002. Tamil Nadu, India.

*Email: vijayavelfsp@gmail.com

Abstract

FSW was invented at the welding institute (TWI) of the United Kingdom in 1991 as a solid-state joining technique and was initially applied to aluminium alloys. Friction Stir Processing (FSP) is an adaptation of friction stir welding with the following unique features: Low amount of heat generation, extensive plastic flow of material, very fine grain size in the stirred zone, healing of flaws and casting porosity, random orientation of grain boundaries in the stirred region, mechanical mixing of the surface and subsurface layers, Therefore, the FSP can be used as a generic process to modify the microstructure and change the composition, at selective location. In FSP, the effect of pin profile on material flow, material mixing, material consolidation is predominant than other parameters. Hence, in this work, the effect of pin volume ratio (dynamic volume/static volume) on microstructural characteristics of aluminium based metal matrix composites was characterized. Microhardness of FSP region was measured and correlated with respective microstructural characteristics. From this investigation, it is found that pin volume ratio of 1.15 exhibited defect free stir zone with higher hardness compared to other ratios. The reasons for the above effects are discussed in detail in this paper.

Key words: Metal Matrix Composites, Friction Stir Processing, Pin Volume Ratio, Microstructure,

Tensile Properties, Micro hardness, Wear Characteristics.