Effect of Filler Wire Type on the Microstructure and Mechanical Properties of Cold Metal Transfer Wire-Arc Additively Manufactured HSLA Steel Cylinders

B. Prabhakaran*, P. Sivaraj, S. Malarvizhi, V. Balasubramanian

Centre for Materials Joining and Research (CEMAJOR), Department of Manufacturing Engineering, Annamalai University, Annamalai Nagar, Chidambaram, India-608002.

Corresponding author Email: rsamuniv2021@gmail.com

Wire-arc additive manufacturing (WAAM) has emerged as a promising technique for fabricating large and complex components with high deposition efficiency, low production cost, and superior buy-to-fly ratios compared to conventional and other additive manufacturing processes. However, limited studies have focused on the influence of filler wire on properties of WAAM-processed high-strength low-alloy steels. In this study, two cylindrical components were fabricated using solid wire (SW) and metal-cored wire (MCW) under an interlayer temperature of 150°C.

Microstructural characteristics and mechanical properties were examined at the top and bottom regions of each cylinder. Owing to variations in thermal gradients during deposition, the top regions exhibited equiaxed grains, whereas the bottom regions contained columnar grains. The average grain size in the SW component was 20.3 μm (top) and 10.7 μm (bottom), while the MCW component showed finer grains of 10.2 μm (top) and 4.7 μm (bottom). The refined microstructure in the MCW-deposited component is attributed to its short-circuit transfer mode in cold metal transfer (CMT) technology and lower heat input. Correspondingly, mechanical testing revealed higher yield strength (YS) and ultimate tensile strength (UTS) in bottom regions of both the components. The MCW-deposited component yielded UTS of 951 ± 26 MPa, approximately 18.2% higher than that of the SW-deposited component. Similar trends were observed in the top regions. The enhancement in strength primarily arose from solid solution strengthening, grain boundary strengthening, and dislocation strengthening mechanisms. These aspects were discussed in the paper

Keywords: Metal-cored wire; Cold metal Transfer; Wire-arc additive manufacturing; High strength low-alloy steel. Mechanical Properties, Microstructural Characteristics