Studies on Properties of Rotating Arc GMA Weldments of 316LN stainless steel

B. Arivazhagan1* and P. Sathiya2

1Materials Joining Section, MMG, IGCAR, Kalpakkam 603 102

*Assistant Professor (Engineering Sciences), HBNI, Kalpakkam 603 102

2Professor, Dept. of Production Engineering, NIT, Trichy 620 015

E-mail:  arivu@igcar.gov.in

ABSTRACT

Type 316 L(N) stainless steel is one of the major structural material for the sodium cooled fast reactor at kalpakkam. Rotating arc also known as spin arc welding is a mode of GMAW process. In this process, the arc was mechanically rotating at various speeds. This process has simple edge preparation with high productivity hence this process can be used to join plates of more than 5 mm thickness.  In the present work, 316L(N) plates of 12 mm thickness were used in the preparation of weld joints. The parameters were optimized to obtain weldments that are visually acceptable as well as radiographic quality. Ferritscope measurement shows that the weld has delta ferrite content in the range of 4.5 FN to 5 FN.  The tensile properties are: UTS: 595 MPa; YS: 380 MPa. The weld has higher strength than other zones of weldments as indicated by Vickers microhardness survey. By varying the speed of arc rotation, it is possible to obtain increased productivity in plates of higher thickness. The distortion of weldments after the welding was found to be minimum due to narrow groove as well as square edge preparation. The average impact energy of the welds was found to be 160 Joules at room temperature. Further studies show that this process offers the scope to improve the productivity of 20 mm thick plates.

Key words: spin arc welding; 316LN; Microstructure