Influence of Friction Stir Processing on the Mechanical, Tribological, and Corrosion Behavior of Mg-1Er-1Pr alloy

Selvakumar Duraisamy1, P. Sathiya1* & R. Vaira Vignesh2

1Department of Production Engineering, National Institute of Technology, Tiruchirappalli, Tamil Nadu-620015, India

2Department of Mechanical Engineering, Amrita School of Engineering, Coimbatore-641112, Amrita Vishwa Vidyapeetham, India

Abstract

Magnesium-rare earth alloys are low-density materials that serve as promising options for lightweight applications. This study investigates the effect of friction stir processing on the mechanical, tribological, and corrosion properties of a Mg-1Er-1Pr alloy. Microstructural analysis, micro-tensile tests, and micro-hardness measurements were carried out to evaluate the mechanical properties. In addition, ball-on-plate wear tests, potentiodynamic polarization, and static immersion corrosion tests were conducted to evaluate the tribological and corrosion behavior of the processed samples. The results show that employing two FSP passes leads to significant grain refinement in the stir zone due to dynamic recrystallization and particle-stimulated nucleation. EBSD results indicated that single-pass FSP refined the grain size from ~243 µm to ~53 µm, while double-pass FSP further reduced it to an average of ~15 µm. The microhardness of the stir zone increased from 56 HV (P1) to 62 HV (P2) compared to the base material. Furthermore, the coefficient of friction (COF) decreased with an increasing number of FSP passes. The corrosion behavior of the FSP-treated samples also showed improved corrosion resistance compared to the base material. Overall, the results indicate that FSP significantly enhances the mechanical, tribological, and corrosion properties of the Mg-1Er-1Pr alloy.

Keywords: FSP, Mg alloys, Microstructure, Tribology, Corrosion