Microstructural and Mechanical Characterization of P91 Steel Weld Joint Produced by A-TIG+TIG Hybrid Process

Gopa Chakraborty*, P. Vasantharaja, Hemant Kumar, C. R. Das, A. Moitra, M. Vasudevan

Metallurgy & Materials Group, Indira Gandhi Centre for Atomic Research, Kalpakkam-603102

*Tel.: +91 44 27480118, e-mail address: gopa_mjs@igcar.gov.in

Abstract

Modified 9Cr-1Mo (P91) steel is extensively used as material for steam generator of thermal and nuclear power plants due to its superior high temperature creep strength and good thermal conductivity. Shielded Metal Arc Welding (SMAW) and Tungsten Inert Gas (TIG) welding are commonly employed processes during fabrication of the steam generator. However, SMAW welds often exhibit reduced impact toughness owing to non-metallic inclusions, whereas TIG welding, though capable of producing cleaner welds with better mechanical properties, is limited by shallow penetration in single-pass applications. Activated TIG (A-TIG) welding addresses this limitation by using a surface-active flux to enhance penetration through arc constriction and surface tension reversal. However, flux application in components with complex geometries can hinder productivity. This study proposes a hybrid welding approach combining single-pass A-TIG followed by TIG welding to reduce the number of TIG passes and improve overall efficiency.

In the present study, a weld joint of 12 mm thick P91 steel plate was fabricated using a hybrid approach combining A-TIG and conventional TIG welding techniques. Microstructural analysis revealed the presence of delta ferrite along the martensitic lath boundaries on the A-TIG side, whereas no delta ferrite was observed on the TIG side. Post-weld heat treatment (PWHT) resulted in marginally higher hardness in the A-TIG weld metal compared to the TIG counterpart. The weld joint exhibited satisfactory mechanical properties, with a tensile strength of 630 MPa and Charpy impact toughness of 120 J. The average oxygen content and volume fraction of inclusions in the weld metal were found to be 340 ppm and 0.02%, respectively. Three-point bend testing yielded peak loads of 2.7 kN (ATIG+TIG), 2.4 kN (A-TIG), and 3.3 kN (TIG), with the higher load on the TIG side attributed to its finer martensitic microstructure and absence of delta ferrite and inclusions. Digital Image Correlation (DIC) strain mapping indicated preferential crack propagation toward the A-TIG weld metal. Impression creep testing further demonstrated superior creep resistance in the TIG weld metal, with lower total creep strain and creep strain rate compared to the A-TIG side. The weld joint produced using the A-TIG and TIG hybrid welding technique demonstrates mechanical properties closely matching those of the TIG-welded P91 steel joint. Studies revealed the suitability of this method for efficiently joining thicker sections of P91 steel while maintaining high productivity and optimum mechanical properties.

Keywords: Modified 9Cr-1Mo steel; hybrid welding; Activated-TIG welding; tensile strength; impact toughness.