Process strategies for building large-volume overhanging Aluminium alloy structures with arc-wire directed energy deposition process

Savyasachi Nellikode1, Akash P Balakrishnan1, J.V. Tilak Kumar1, Sherin Thampi1, Murugaiyan Amirthalingam1

[1] Department of Metallurgical and Materials Engineering, Indian Institute of Technology Madras, India

Corresponding author murugaiyan@iitm.ac.in

Abstract

This study aims to develop process strategies for fabricating large-volume aluminium alloy walls with straight, inclined, overhanging, and curved geometries using arc-wire directed energy deposition (AW-DED) also known as wire and arc additive manufacturing (WAAM) process. To minimize porosity and geometric distortion during thick wall build-up, two different fabrication methods were proposed: (i) by varying the torch orientation and (ii) by tilting the substrate (turn-table) while maintaining a fixed vertical torch. A robotic AW-DED system equipped with a Fronius CMT process was utilized to deposit ER5183 aluminium alloy walls with designed inclination angles and complex curvature. In the first approach, the torch angle was dynamically adjusted based on the local slope of the build surface to manipulate the molten pool flow direction. In the second approach, the same wall geometries were produced by tilting the substrate instead of the torch, thereby maintaining consistent droplet transfer behavior and arc stability. The effects of these two methods on bead morphology, layer uniformity, porosity, and heat accumulation were systematically investigated. Both strategies enabled stable deposition of overhanging and curved walls without support structures. The substrate-tilt method provided smoother layer stacking, reduced lateral spreading, and improved surface definition, while the torch-tilt method offered better adaptability for steep overhangs. A curvature-adaptive path planning algorithm and energy-modulation scheme (−10 % heat input on up-slopes) were further introduced to improve bead consistency and reduce pore formation. This work demonstrates the feasibility of producing thick and geometrically complex aluminium walls using WAAM without auxiliary support by combining process control and geometric compensation to produce near-net-shape aluminium fabrication.

Keywords: Arc-wire directed energy deposition (AW-DED), Aluminium Alloy, Overhanging Structure, Substrate Tilting, Torch Orientation, Molten Pool Control, Path Planning.