Effect of Rotation Speed and Friction Pressure on Micro-structure and Mechanical Properties of Rotary Friction Welded Low Alloy Steel Tube Joints

- Selvaraja*, K. Shanmugamb, P. Selvarajc, Prasanna Nagasai d, V.Balasubramaniand

a,b,,dCentre for Materials Joining and Research (CEMAJOR), Department of Manufacturing Engineering, Annamalai University, Annamalainagar

cDepartment of Mechanical Engineering, MAM College of Engineering and Technology, Tiruchirappalli, India.

E Mail : premaselvaraj.mkk@gmail.com

Abstract

Low alloy steel (LAS) properties make it ideal for use in oil field services, petrochemical plants, refineries, and power plants where gases and fluids are transported at high pressures and temperatures. The thermal conductivity of LAS varies from that of carbon and stainless steel. Differences in the coefficient of thermal expansion and thermal conductivity may cause issues when welding various materials (from LAS-drawn to forging). These variations put extra strain on the joint. Therefore, it is possible for a dissimilar metal weld to deform or go out of alignment. The strains produced by variations in temperature (expansion and contraction) can also result in cracking if they are stronger than the strengths of the two materials. When welding LAS, the choice of filler metals is equally crucial.

Rotary Friction Welding (RFW) is a solid-state welding process that is becoming increasingly popular due to advantages such as low weld heat input, high production efficiency, ease of manufacture, and environmental friendliness. Rotary friction welding can weld materials that are difficult to fuse using fusion welding techniques. Hence, the present investigation is carried out to study on the effect of process parameters such as rotating speed and friction pressure on the micro-structure and mechanical properties of LAS joints using RFW.

The experimental results indicate that rotating speed and friction pressure play major role on the tensile strength of the joints. The results show that the tensile strength of the friction-welded specimens increased with the increasing rotation speed to 60 rps and friction pressure reaching 0.84 MPa/s and decreasing for further increases in rotating speed and the friction pressure. In comparison to the PDZ, HAZ, and base metal, hardness measurements reveal a higher hardness at the weld (FDZ) center due to favorable micro structural characteristics.

Keywords: Rotary friction welding, Low alloy steel, Rotating Speed, Friction pressure, Mechanical properties, Micro-structure