Development of Stellite-6 hardfacing on the stainless steel foot of the FBTR control rod using laser surfacing technique

Shobhit Verma* , Hemant Kumar, M. Elango, S.K.Prasad, G. Ramesh, S.Sridhar

Indira Gandhi Centre For Atomic Research, Kalpakkam - 603102, India

*Corresponding author: Shobhit verma, shvr@igcar.gov.in

Abstract:

This study aims for a low-heat-input laser deposition (laser cladding) route was developed and qualified for Stellite-6 overlays on SS316 control-rod foot intended for the Fast Breeder Test Reactor (FBTR). A continuous-wave fiber laser with coaxial powder delivery and argon shielding was employed in two variants: single-layer deposition at 1650 W and double-layer deposition at 2 × 1100 W. Characterization comprised macro- and microstructural examination, HV0.3 line-hardness traverses from the coating surface into the substrate, and dimensional mapping on a 50 mm grid before and after heat treatment. Process development prioritized distortion control to minimize corrective stock removal while preserving overlay thickness. Although minor bend during deposition was observed which can lead to uneven coating thickness, final coating uniformity and straightness were achieved by cylindrical grinding; production records showed restoration to drawing limits without loss of metallurgical bond or adverse change in hardness response. Deposits exhibited sound bonding with no cracking or lack-of-fusion, and the etched interpass band was identified as a good bonding between substrate and coating. The coating sustained approximately 500–600 HV to ~0.70 mm depth, followed by a smooth transition to ~155–223 HV at 1.50 mm, consistent with limited dilution under low thermal input. Dimensional measurement after heat treatment and finish grinding confirmed good straightness (~0.05–0.13 mm) and low bend, with representative peak-to-peak deviation relative to a 20.900 mm reference ≤ 0.172 mm. These results demonstrate that a carefully constrained, low-heat-input laser deposition window, combined with calibrated cylindrical grinding, yields uniform, production-grade overlays suitable for FBTR control-rod service.

Keywords: Hardfacing; stainless steel; stellite-6; laser deposition, wear, distortion