“INFLUENCE OF FRICTION PRESSURE ON MECHANICAL PROPERTIES AND MICROSTRUCTURAL CHARACTERISTICS OF MARAGING STEEL- 250 JOINTS USED IN  AERO ENGINES”

*B.Saravanan1, K.Shanmugam2, V.Balasubramanian 3,T.Balamurugan4,

123Centre for Materials Joining and Research (CEMAJOR),

Annamalai University, Annamalai Nagar, Chidambaram,India-608002.

4Arasu Engineering College,Kumbakonam,India-612501.

Email:krbsaravana@gmail.com

ABSTRACT

Maraging steel -250 (MS-250) is widely used in various industries such as tooling, aerospace, automotive, military industries. Maraging steel-250 is a high-strength, low-carbon iron alloy which is known for its combination of strength and toughness. An essential part of an aero engine, the low pressure (LP) main shaft rotates at 10,000 rpm while in operation. Currently, fusion welding and mechanical bolting are used to create these LP main shaft assemblies. However, fusion welding of these steels often results in elevated fusion zone temperatures which adversely induces the percentage of reverted austenite in the fusion zone and micro segregation of the alloying elements which deteriorates the toughness of the welds. Solid state welding techniques can be utilized to solve these issues. However, the Rotary Friction Welding (RFW) technology is the only practical way to make cylindrical components like the LP main shaft.

This paper discusses the influence of one of the important RFW parameters,  friction pressure on mechanical properties and microstructure of the friction welded 25 mm diameter Maraging steel-250 (MS-250) joints. The experiments were performed by varying the friction pressure from 0.40 MPa to 0.60 MPa  and   keeping   constant rotational speed, friction time, forging pressure and forging time. The experiments were conducted and the corresponding tensile strength and microhardness survey was carried out across the center line to identify weak region. A detailed microstructural analysis with grain size, fracture surface analysis (SEM) and EDS were performed at the fracture surface for all the joints. It was found that the using joint welded  0.45 MPa welded superior mechanical properties due to the formation of fine grains at the fully deformed zone. The ultimate tensile strength and hardness were found to be 1460 MPa and 277 HV in these joints.

Key words: Maraging steel-250; Rotary Friction Welding; Tensile properties;

Micro hardness and Micro structure.