Incorporating carbide particles in steel using Wire Arc Additive Manufacturing (WAAM): Microstructure and property correlation

Akash Vincent1, Harshavardhana N1*

Department of Mechanical Engineering, SRM Institute of Science and Technology, Kattankulathur, Chengalpattu - 603203, Tamil Nadu, India,

e-mail: harshavn@srmist.edu.in

ABSTRACT

Wire arc additive manufacturing (WAAM) has emerged as a cost-effective route for producing large-scale metallic components; In this work, SS316L walls were deposited using a robotic gas metal arc welding (GMAW) system based on an ABB IRB 1510, with process parameters optimized to achieve stable metal transfer and consistent bead geometry. Welding wire with a diameter of 1.2 mm is used for the fabrication of the wall. Addition of silicon carbide powder into the bead through a narrow cut along the weld direction. Silicon carbide powder with a size of 50-90 microns was used in dispersion. The influence of travel speed, wire feed rate and interlayer temperature on deposition efficiency, microstructure and mechanical performance was investigated. Optical and electron microscopy revealed a fully austenitic matrix with a controlled fraction of δ-ferrite, and the grain size was found to be 300 μm from columnar to equiaxed transition across the build height, governed by local thermal gradients and heat accumulation. The results obtained from mechanical tests and microstructural characterization, show an improvement of 200 MPa in the mechanical properties of the carbide powder-dispersed 316L stainless steel compared to steel without carbide powder dispersed.

Keywords: Wire Arc Additive Manufacturing, Carbide-dispersed Steel.