Repair and refurbishment of high speed steel forging tooling by laser directed energy deposition – role of laser parameters on the interface microstructural evolution

by Anjali Rathish, Nikhil Thawari, Murugaiyan Amirthalingam

Laser Directed Energy Deposition (DED) is an additive manufacturing technique that enables controlled material deposition, precise melting, and strong metallurgical bonding, making it suitable for the repair and refurbishment of high-value components. This capability has become increasingly important as industries face rising replacement costs, long lead times, and the need to extend the service life of critical tooling components. Although L-DED has been successfully applied for H13 tool-steel repair, prior studies report challenges related to microstructural instability, heat-affected zone(HAZ) softening, and cracking when process parameters are not adequately optimised. Further, H13 tool steel exhibits strong sensitivity to thermal gradients and cooling rates during laser deposition, influencing carbide dissolution, retained austenite formation, and residual stress induced cracking. In this study, H13 tool steel was selected due to its wide industrial usage in warm forging dies and its critical demand for reliable repair solutions in industrial practice. The objective of this work was to systematically examine the influence of laser power and scan speed on bead geometry, microstructure evolution, and repair-layer performance of H13 tool steel. Single tracks were deposited using laser powers of 850, 900, and 1000 W at scan speeds of 5, 6, and 7 mm/s, resulting in nine distinct process conditions. Based on bead morphology and track stability two optimal conditions were chosen for multilayer cube fabrication in initial stage. The fabricated cubes were first characterised to study microstructure and hardness. After characterisation, the top surface of each cube was ground for rebuilding. Repair layers were then deposited using the optimised L-DED parameters. The results show that the selected parameters facilitate stable deposition with minimal defects, produce a uniformly refined microstructure, and achieve hardness levels comparable to the substrate. These outcomes validate the effectiveness of L-DED as a dependable method for industrial repair of H13 tool steel.

Keywords: - Laser Directed Energy Deposition; Additive Repair; H13 tool steel; Process parameter optimisation; Microstructure evolution